OVERVIEW

Procedure/ Steps

Materials

- Material samples provided by the instructor

- Paper and pencil

- Safety Glasses

- Oxy-Acetylene torch set

- Cold water

- Tongs

- Rockwell Hardness Tester

- 1/16 in. ball indenter

Steps

- Gather sample material.

- Take 5 measurements from each sample.

- Place sample on RHT.

- Push rear lever all the way back.

Data Collection

| Sample Type | Measurement 1 | Measurement 2 | Measurement 3 | Measurement 4 | Measurement 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| Square Stock | 40 | 41 | 39 | 42 | 35 | 39.4 |
| Hex Stock | 63.5 | 70 | 67 | 70.5 | 60 | 68 |
| Flat Stock | 56.5 | 56.5 | 58.5 | 59 | 58.5 | 57.8 |
| Brass | 37.5 | 37.5 | 42 | 39 | 36 | 38.4 |
| Aluminum | 41 | 39.5 | 42 | 61.5 | 38 | 44.4 |
| Heated Flat Stock | 83 | 60 | 57 | 74 | 68 | 68.4 |

Conclusion

- This section allows you to conclude what you learned, overall, during the laboratory activity. Results should address the following questions:

- DO THE QUESTIONS AT THE END OF THE LABORATORY SHEET

  - Was the laboratory objective accomplished?

  - How did this laboratory activity relate to or support the concepts presented in course content?

Technical Article Correlation

Article: Hardness test methods and hardness conversion tables. British Stainless Steel Association. Retrieved April 6, 2010, from http://www.bssa.org.uk/topics.php?article=97